| Item | Size Range | Attributes | Specification |  | ## Notes |
| --- | --- | --- | --- | --- | --- |
| Supplier | All Products |  | ISO 9001:2015 certified. PED compliant suitable for use with Group 1 Gases. |  |  |
| Pipe Spools & Fittings |  | Performance | Qualification testing to ASTM F1545. Rating Class 150 to full vacuum @ 200oC for up to and including 200NB. Above this size consult manufacturer. |  |  |
| # Pipe Spools –Welded Fabrication | 25NB to 300NB ≤ 150NB Length 100mm to 6000mm 200NB to 350NB Length 200mm to 3000mm | Materials | Carbon Steel pipe to ASTM A106 Grade B / API.5L Grade B. Schedule 40 25NB to 150NB. Schedule 30 200NB and above. Flanges to ASTM A105. Stub Ends to BS1501-161-430A. |  |  |
|  |  | Construction – Welded | One fixed and one rotating flange conforming to ASME B16.5 Class 150. Weld pip positioned to prevent sliding of rotating flange. |  |  |
| # Pipe Spools – Van Stone | 25NB to 200NB ≤ 100NB Length 250mm to 6000mm 150NB Length 500mm to 6000mm 200NB Length 500mm to 3000mm |  | Carbon Steel pipe to ASTM A106 Grade B / API.5L Grade B. Schedule 40 25NB to 150NB. Schedule 30 200NB. Flanges to ASTM A105. |  |  |
|  |  | Construction – Van Stone | Two swaged ends with rotating flanges conforming to ASME B16.5 Class 150. Weld pips positioned to prevent sliding of rotating flanges. |  |  |
| Pipe Spools – All types |  | Venting – Materials & Construction | 5mm vent holes, with welded carbon steel vent bosses threaded 1/4in BSP and PTFE Plugs also with 5mm hole. >=500mm Length one vent hole. Lengths longer than 500mm two vent holes at the same place on the circumference. |  |  |
|  |  | Vent Extensions – Materials & Construction | Carbon steel Schedule 80 threaded 1/4in BSP 75mm long screwed into threaded ¼” BSP welded boss positioned over vent hole. |  |  |
|  |  | Earthing | To customer specification |  |  |
|  |  | Materials – finish | Manufacturer’s standard primer over a grit blasted surface to a cleanliness of SA 2.5. |  |  |
| Pipe Liner – Virgin PTFE | 25NB to 300NB | Materials | PTFE to ASTM D1457 Type III or ASTM D4895 or ASTM D4894. Note pipe liners made by Ram extrusion and tape wrapping are not permitted, whilst those manufactured by isostatic moulding are not preferred. Minimum Tensile Requirements UTS 20,7MPa Elongation at Break 250 % in both directions. Specific Gravity in the range 2,14 – 2,19 |  |  |
|  |  | Construction | Nominal Wall Thickness (mm) | Superweight Nominal Wall Thickness (mm) |  |
|  | 25NB |  | 3.2 | 4.5 |  |
|  | 40NB |  | 3.2 | 4.5 |  |
|  | 50NB |  | 3.2 | 4.5 |  |
|  | 80NB |  | 3.2 | 4.8 |  |
|  | 100NB |  | 4.5 | 5.0 |  |
|  | 150NB |  | 5.5 | 6.0 |  |
|  | 200NB |  | 8.5 |  |  |
|  | 250NB |  | 9.1 |  |  |
|  | 300NB |  | 10.4 |  |  |
|  | 350NB |  | 8.3 |  |  |
| Pipe Liner – all |  |  | Interference fit liner, flared both ends to raised face diameter. |  |  |

| Item | Size Range | Attributes | Specification | ## Notes |
| --- | --- | --- | --- | --- |
| Spacers | 25NB to 300NB Length 30mm to 100mm | Materials | Stub End & Steel tube - Carbon Steel to BS1501-161-430A Pipe - Carbon Steel to ASTM A106 Grade B / API.5L Grade B Liner - PTFE to ASTM D1457 Type III or ASTM D4895 |  |
|  |  | Construction | Type 1 Solid PTFE – max length 25mm Types 2 & 3 PTFE lined carbon steel |  |
| # Fittings – All types | 25NB to 350NB standard, larger sizes to order Centreline to face and face to face dimensions as ASME B16.5 Class 150 where applicable. | Range | 90 Degree Elbows 45 Degree Elbows Equal Tees Reducing Tees Instrument Tees Short Branch Equal Tees Lateral Tees Concentric Reducers Eccentric Reducers Reducing Flanges Crosses Blank Flanges |  |
| Fittings – Castings |  | Materials | Cast Steel to ASTM A216 Grade WCB. |  |
|  |  | Construction | Fixed flanges or welded cast construction rotating flanges. |  |
| Fittings – Fabrications |  | Materials – Bends | Cast Steel to ASTM A234 WPB |  |
|  |  | Materials – Plate | BS1501-161-430A |  |
|  |  | Materials – Flanges | ASTM A105 |  |
|  |  | Materials – Pipe | Carbon Steel to ASTM A106 Grade B / API.5L Grade B |  |
|  |  | Materials – finish | Manufacturer’s standard primer over a grit blasted surface to a cleanliness of SA 2.5. |  |
|  |  | Construction | Fixed or Rotating as specified |  |
| # Fittings – All types | PTFE Lined fittings only | Venting – Materials & Construction | ≤ 150NB 5mm vent holes, with welded carbon steel vent bosses threaded 1/4in BSP and PTFE Plugs also with 5mm hole. |  |
|  | All fittings | Vent Extensions Materials & Construction | Carbon steel Schedule 80 threaded 1/4in BSP 75mm long screwed into threaded ¼” BSP welded boss positioned over vent hole. Steel reducing fitting fitted to injection boss on PFA fittings to accept 1/4in BSP vent extension. |  |
|  |  | Earthing | To customer specification | iii |
| Fittings – Blank Flanges | 25NB to 600NB | Materials & Construction | Flanges to ASTM A105. Virgin PTFE sheet etch bonded. Lined to raised face. Liner thickness: 4mm |  |
| Fittings Lining – PFA/PTFE | 25NB to 300NB | Materials | PFA to ASTM D3307 type II Minimum tensile properties 26MPa and 300% Elongation at Break. PTFE to ASTM D1457 Type III or ASTM D4895 or ASTM D4894 minimum properties as pipe lining. Note PFA is the preferred lining material, with paste extruded PTFE liners also acceptable. Fittings manufactured by isostatic moulding are to be excluded where practical. |  |
| Fittings –All |  | Vent Extensions – Materials & Construction | Carbon steel Schedule 80 threaded 1/4in BSP 70mm long screwed into threaded ¼” BSP welded boss positioned over vent hole. |  |
| Identification |  |  | Nominal bore size and length to be marked indelibly on pipe spools. Supplier order number and line item number and customer name on end boards of pipe spools, Supplier order number and line item number on end caps for fittings. |  |

| Item | Size Range | Attributes | Specification | ## Notes |
| --- | --- | --- | --- | --- |
| In Process Testing |  | PTFE | Visual Outside Diameter Wall thickness (4 positions) Acceptable sintering profile Longitudinal Tensile Strength Transverse Tensile Strength Longitudinal Elongation at Break Transverse Elongation at Break SG determination of PTFE |  |
| Finished Product Testing |  |  | Electrostatic Test @ 20kV Hydrostatic Test @ 29 Bar g |  |
| Packaging – All products |  |  | Water resistant MDF or similar end boards bolted to the flange face for PTFE lined products. Plastic end caps for PFA lined products. |  |
| Special Requirements |  |  | To contract definition |  |
| Certification |  |  | Standard certificate of conformity provides details of materials used and details of Electrostatic Test and Hydrostatic Test |  |
| Project Documentation |  |  | To customer requirement |  |
| Traceability |  |  |  |  |

The vent bosses and PTFE plugs are specified for permeant services.  Otherwise these can be omitted and the items would be supplied just with vent holes.

? These vent bosses and extensions are for taking the vent hole through insulation.  They are supplied taped to, but not fitted to the spool to prevent damage in transit.  They can be omitted for non-insulated liners.

Earthing of lined piping is advised as the flare faces are an insulating item.  Choices are star washers on bolting, earthing studs or lugs with copper earth bonding straps.  For rotating flanged items, the flange can be earthed using “Spikies” or additional studs or lugs.  For wafer fittings, such as instrument tees studs or lugs should be specified.

Note PTFE to ASTM D1457 Type III or ASTM D4895 are specifications for fine powders for paste extruded PTFE, whilst ASTM D4894 is a granular PTFE standard for Isostatic moulding grades of PTFE

Superweight liner can be specified for permeant services.

? Type 1 – Solid PTFE.  Types 2 – PTFE lined thick walled steel tube and Type 3 – PTFE lined steel tube with stub ends.

Note, Instrument Tees are not included in ASME B16.5, check manufacturers dimensions.  25NB 45 degree elbows are threaded UNC ½in.  The 100NB x 50NB Instrument Tee has a branch diameter of 40NB, but a 50NB flange.

Must be specified at the time of ordering.  Supplied taped to, but not fitted to the spool.

Where identification of isometric drawing and revision number are possible these are marked on each spool or fitting or ID tag as appropriate.

Additional requirements include: special paint finishes, certification of testing of lining, stainless steel spools & fittings, BS or DIN flanges, fittings with rotating flanges, special low temperature service requirements.

The following documentation can be supplied as evidence of quality control: Quality Plan, Product Drawings, Weld Procedures, Welder Qualifications, NDE Procedures, NDE Operator Qualification, Material Certification (2.2 or 3.1) and Certificate of Conformance.

? All products should be reverse traceable from component through the manufacturing process to original polymer certification.  This is provided on fittings via a unique number stamped upon the component flange and on pipe spools via the PTFE run reference stamped upon the component flange.  All records relating to the manufacture and test of these items shall be available for scrutiny.